## Slide 1
WG2 co-chairs:
M.Gorelik, Chief Scientist for Fatigue and Damage Tolerance, FAA
A.Fischersworring-Bunk, Senior Consultant, Structures, MTU AeroEngines
2024 FAA - EASA AM Workshop
WORKING GROUP 2:
Fatigue and Damage Tolerance (F&DT) and Non-Destructive Inspection (NDI) Considerations for Metal AM
General Session Briefing
Sept. 19, 2024

## Slide 2
WG2 Briefing – 9/19/24
Key Objectives of the WG2:
To identify key standardization gaps
  Providing guidance to AM design and Q&C community
  An opportunity to develop a design handbook for AM? Who would do it? (e.g. AIA AM WG, SAE G-37, ..?)
A concise description of why metal AM is different from “conventionally” manufactured metallic parts (wrought, cast, PM, etc.)
  Some information is already available from various sources
To identify key technology gaps
Recommendations for enabling R&D

## Slide 3
Discussion Topics
Topic 1. F&DT methodologies for “B+ class” parts
“B+ class” notionally defines either safety-critical parts, or part that are considered fatigue-sensitive and F&DT analysis typically performed by OEMs regardless of regulatory requirement
  Use of probabilistic methods (e.g. defects statistics for DT assessment) + NDI capabilities.
  Context: inherent anomalies (model-based correlation between anomaly populations and part performance).
    Not a standard / mandatory approach, just one of the analysis options in the “toolbox”
    What are acceptable methods of showing “equivalence” of anomaly distributions (e.g. direct characterization methods vs. QA / inspections)? Potential for using production / QA data for periodic updating.
WG2 Briefing – 9/19/24

## Slide 4
Discussion Topics (cont.)
Topic 2. Statistics of Anomalies (implications are not limited to just high-criticality parts)
  Each anomaly morphology type may require its own distribution (e.g. gas porosity vs. LOF) – different underlying physics. Statistics may also need to be location / zone specific.
  Need to assess the average frequency of occurrence (one of the two elements of exceedance curves)
    For relatively high frequency of volumetric anomalies – can use direct measurements, e.g. CT (may need to combine different resolution scales of CT) or metallography (see also the last bullet below).
    Another option - calibration of exceedance curves with in-service experience (not feasible near-term)
  Additional consideration: need to introduce spacing criterion or metric (e.g. for anomaly clusters)
  How sophisticated should statistical distribution(s) be? Need to keep in mind that this provides input into Fracture Mechanics (FM) based analysis tools. Majority vote – 2D FM is sufficient (context - inherent anomalies).
    Recommendation: to use univariate / unimodal distributions as much as practical
  May need to consider a “transfer function” – to convert more detailed 3D information into 2D description consistent with 2D FM analysis assumptions. However, 1D approximation (e.g. Murakami, max length, etc.) is deemed sufficient for most cases within this framework.
WG2 Briefing – 9/19/24

## Slide 5
Discussion Topics (cont.)
Topic 3. Uninspectable areas of high-criticality parts (context: rogue flaws)
  Have to rely on special process controls (i.e. “product of the process” approach)
  Max allowable flaw size based on deterministic FM analysis
  Functional / component-level tests (cannot address every area in a part, especially for high geometric complexity designs)
  Note: if it’s a design-limiting area – should be inspectable per certain regulations (e.g. §25.571)
WG2 Briefing – 9/19/24

## Slide 6
Discussion Topics (cont.)
Topic 4. Potential use of in-situ process monitoring (ISPM)  needs to be coordinated with WG3
  As an alternative to conventional NDI – contingent upon technology maturation and validation
  As a supplement to conventional QA system
  Can be a sensitive gage for process stability (or a lack of thereof, i.e. process deviations)
  Could potentially distinguish between two classes of ISPM –
    main class to be used to detect process deviations;
    a more narrow class – to potentially detect location-specific defects formation (e.g. rogue defects); would require additional development work to quantify detection capabilities
  Focus area – use of this technique for part zones uninspectable using conventional NDI, as well as for undetectable types of anomalies
    To be used as an enhancement to conventional process control (specific to uninspectable region / zone within the part)
    Even if it’s feasible, need to keep in mind potential effects of post-processing steps, so the final NDI would still likely be required, as well as in-service inspections
WG2 Briefing – 9/19/24

## Slide 7
Discussion Topics (cont.)
Topic 5: Transition from material allowables to design values for fatigue
Fatigue material allowables in public domain (i.e. divorced from company-specific lifing system) have value, but are currently not viable for design work
Potential value – to establish process equivalency, isolate variability to just intrinsic material properties (base of the test pyramid)
Additional considerations – standardization of test methods, buy-in methods (for a specific process / machine / etc.), standardization of S-N data statistical modeling methods (both for nominal and min properties), definition of test matrices (including number of heats / lots / etc.)
WG2 Briefing – 9/19/24

## Slide 8
Recommendations for the WG2 path forward
To convert this standing WG2 into a sub-committee or a task group associated with a well-established SDO (specific organization to be defined later).
Initial target – to develop a technical white paper reflecting on the cumulative results of the WG2 proceedings over the past few years. Initial target – to develop a draft document by the time of the 2025 Cologne EASA – FAA AM Workshop.
Reached an initial consensus among the WG2 members in attendance (F2F + virtual).
WG2 Briefing – 9/19/24